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Product Information
Copper Phosphorus CP2 Brazing Rods
Brand: Super 6
Product Description
Super 6 CP2 Brazing Rods are high-quality phosphorus-deoxidised copper rods specifically designed for gas welding and brazing of copper and copper alloys. With a low melting point and excellent capillary action, CP2 rods provide clean, leak-free joints ideal for plumbing, HVAC, refrigeration, and general copper fabrication work. These bare rods require no additional flux when brazing copper to copper, simplifying the brazing process and reducing cleanup.
Key Features
· Phosphorus copper alloy for excellent thermal and electrical conductivity
· No flux required for copper-to-copper brazing self-fluxing
· Low melting range ideal for precise capillary brazing with minimal heat input
· Smooth flow characteristics for neat, strong joints with minimal effort
· Supplied in convenient 1kg tube packs, suitable for on-site or workshop use
Typical Applications
· Plumbing and HVAC installations
· Refrigeration systems
· Copper pipework and fittings
· Electrical conductor brazing
· General-purpose copper and brass fabrication
Chemical Composition (% by weight)
	Element
	Typical Content

	Copper (Cu)
	Approx. 98 – 99%

	Phosphorus (P)
	Approx. 0.7 – 1.1%

	Other
	≤ 0.5%





Physical and Technical Data
	Property
	Value

	Melting Range
	Approx. 710 – 780°C

	Recommended Brazing Temperature
	680 – 760°C

	Flux Type
	Bare rod (self-fluxing on copper)

	Suitable Brazing Methods
	Oxy-acetylene, torch

	Joint Strength
	High, leak-proof joints


Safety and Handling
· Use in well-ventilated areas to avoid inhaling fumes
· Always wear appropriate PPE, including gloves and safety goggles
· Follow all applicable health and safety regulations during use












Liability Notice: Whilst all reasonable efforts have been made to ensure the accuracy of the information contained, this information is subject to change without notice and can be only considered as suitable for general guidance.
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